MAGNETIC AND STRUCTURAL PROPERTIES OF SOME GLASSES CONTAINING RARE EARTH IONS WITH APPLICATIONS IN TELECOMMUNICATIONS

CULEA EUGEN and GOG LIDIA

Physics.Dept., Technical University of Cluj-Napoca,

Str.C.Daicoviciu nr.15, 3400 Cluj-Napoca, Romania

The xR2O3(1-x)[(1-y)Na2B4O7.yMO] vitreous system with R=Nd, Gd, Dy and Ho, MO= Al2O3 or PbO, y=0 or 0.05 and x = 0.01÷0.25 were prepared and studied magnetic susceptibility and density measurements. Magnetic susceptibility data indicate a Curie-Weiss type magnetic behaviour of the samples. Density data suggest that the rare earth ions play a network modifier role in the studied glass matrices. Al2O3 shows an anticlustering effect in the case of glasses containing holmium ions.

1.Introduction

Glasses containing rare earth (RE) ions constitute the ideal material for obtaining the main elements of the equipment used in telecommunications (lasers, amplifiers, and optical fibers) [1-3]. One of the most important requirements concerning the laser active elements is to contain a high level of RE ions in order to ensure a high level of the laser power. However, the increase of the RE ion concentration is limited by the clustering tendency of these ions, which occurs at relatively low concentration. To follow the evolution of the clustering mechanism with respect to the RE ion concentration and the possible anticlustering effects of some additives, we studied some borate glasses containing Nd, Gd, Dy and Ho ions and two additives, namely Al2O3 and PbO, using magnetic susceptibility and density measurements. The mentioned rare earth ions were choosen because previous reports (Nd [4, 6], Gd [7-11], Dy [12] and Ho [13, 14]) show that they appear in the oxide glass matrices in a single valence state, namely RE 3+.

2.Experimental

Samples of the xR2O3(1-x)[(1-y)Na2B4O7.yMO] vitreous system (noted xRNM) where R=Nd, Gd, Dy and Ho, MO= Al2O3 or PbO, y=0 or 0.05 and x = 0.01, 0.05, 0.10, 0.15, 0.20 and 0.25 were obtained using reagent grade Na2B4O7.10H2O, PbO and Nd2O3. Appropriate amounts of Na2B4O7 glass powder, Al2O3 or PbO and RE oxide were mixed and melted at 1000oC for 15 minutes. The melts were quenched on a refractory steel block.

Magnetic susceptibility measurements were performed on a Faraday type balance in the 80-300K temperature range. Density measurements were performed using the picnometric method with water as the reference immersion liquid.

3.Results and discussion

The magnetic behaviour of the xRNM glasses was assumed to be due to the presence of the RE ions. The experimental magnetic susceptibility data obtained for the xRNM glasses were corrected taking into account the diamagnetic contribution of the host glass matrices.

The thermal variation of the inverse magnetic susceptibility was linear for all the samples. Fig.1 presents the thermal variation of the inverse molar magnetic susceptibility, (m-1, of xRNM glasses, where R=Nd. This figure is representative for all the samples of the xRNM vitreous system and indicate a Curie type behaviour for the samples with x(xcr and a Curie-Weiss type behaviour for x( xcr, described by

(m-1 = (T-(p)/Cm					 (1)

where Cm is the molar Curie , (p is the paramagnetic Curie temperature and xcr=0.03-0.10 depending on the rare earth ion type.

Fig.1: Temperature dependence of the inverse magnetic susceptibility of xRNM glasses with R=Nd, MO=PbO, y=0.05 and x=0.05(■), 0.10((), 0.15(●), 0.20(○) and 0.25(▲).

Fig.2 presents the composition dependence of the paramagnetic Curie temperatures,(p, of the xRNM glasses. Note the small and negative values obtained for (p.

The analysis of magnetic data for xRNM glasses suggests that for the glasses containing small amount of RE oxide (x(xcr) the magnetic RE3+ ions are isolated and no magnetic order is present. The glasses with x( xcr present a mictomagnetic type behaviour [15], where both isolated and exchange coupled RE magnetic ions are present in the glass matrix. As suggested by the small negative (p values, the exchange interactions between the RE3+ ions are weak and predominantly antiferromagnetic.

Fig.2: Composition dependence of the paramagnetic Curie constant, (p, of the xRNM glasses with y=0, R=Nd (◊), Gd(■), Dy(▲) and Ho (x).

The magnetic data obtained for the xRNM glasses are in agreement with the data previously reported for other oxide glasses containing the same RE ions [5-14] and were summerized in Tabel 1.

Table 1:

Magnetic data of xRNM glasses.

| R (RE ion) | x | Electronic configuration | Magnetic behaviour | Paramagnetic Curie temperature (p |
| --- | --- | --- | --- | --- |
| Nd 3+ | 0.01-0.25 | 4f 3 | Curie-Weiss xcr=0.10 | 0( /(p/ ( 26 K |
| Gd 3+ | 0.01-0.20 | 4f 7 | Curie-Weiss xcr=0.05 | 0( /(p/ ( 6 K |
| Dy 3+ | 0.01-0.15 | 4f 9 | Curie-Weiss xcr=0.03 | 0( /(p/ ( 6 K |
| Ho 3+ | 0.01-0.20 | 4f 10 | Curie-Weiss xcr=0.10 | 0( /(p/ ( 22 K |

Fig.3 shows the compositional variation of the density for the xRNM glasses. A simple inspection of the data presented in this figure suggests that all the studied RE ions exerted a network modifier role in the host glass matrices.

Fig.3: Composition dependence of the density of xRNM glasses with y=0, R=Nd(●), Gd(▲), Dy(() and Ho(■).

Fig.4: Influence of the additives on the composition dependence of the paramagnetic Curie constant, (p, for the xRNM glasses with R=Ho, y=0((), y=0.05 and MO=PbO(■), and

y=0.05 and MO=Al2O3(▲).

Fig.4 presents the compositional variation of the paramagnetic Curie temperature xRNM glasses with R=Ho and M=0, Pb and Al. The data from this figure suggests a weak anticlustering effect of the aluminium oxide in the case of the holmium ions. For all the other samples the influence of the additives was neglectible.

Conclusions

Magnetic data indicate that the magnetic behaviour of xRNM glasses is of a Curie-Weiss type. For samples with small amounts of RE ions (x(xcr) they appear as isolated species, while for higher amounts of RE ions (x( xcr) a mictomagnetic behaviour, due to the presence of both isolated and coupled species, was observed. Al2O3 shows an anticlustering effect in the case of glasses containing holmium ions.

# REFERENCES

1. CLARE A., in Rare Elements in Glasses, Key Engineering Materials, edited by J.E.SHELBY, Vol.94-95  (Trans. Tech. Publications) 1994, pp.161-181.

2. PARADIS P.F., BABIN F., GAGNE J.M. and LEVESQUE S., J.Opt.Soc.America, B14 (1997) 1009.

3. DAWAR A.L., MEHTA V. MANSINGH A. and RUP R., Optical Mater. 22 (1997) 33.

4. MOORJANI K. and COEY J.M.D, Magnetic Glasses, Elsevier Publishers, Amsterdam, 1984.

5. ARDELEAN I., ILONCA GH. and SEVIANU V., J.Less-Comm.Met.111 (1985) 113.

6. CULEA E. and BRATU I., Acta Materialia  49 (2001) 123-125.

7. NICKLIN R.C., JOHNSTONE J.K., BARNES R.G. and WILDER D.R., J.Chem.Phys., 59 (1973) 1652.

8. ARDELEAN I., BURZO E.,MITULESCU-UNGUR D. and SIMON S.,J.Non-Cryst.Solids 146 (1992) 256.

9. VALENTE M.A. and MENDIRATTA S.K., Phys.Chem.Glasses, 33, 4 (1992) 149.

10. ILIESCU T., SIMON S., MANIU D. and ARDELEAN I., J.Mol.Structure 294 (1993) 201.

11. CULEA E.,POPA. and COSMA I.,J.Magn.Magn.Mat. 157/158 (1996)163-164.

12. CULEA E. and BRATU I., J.Non-Cryst.Solids 262 (2000) 287-290.

13. BURZO E., ARDELEAN I.and MITULESCU D, J.Mater.Sci.Let. 11 (1992) 1496-1497.

14. CULEA E., RISTOIU T. and BRATU I., Mat.Sci.& Engn., B57 (1999) 259.

15. BECK P.A., Metall.Trans, 2 (1971) 2015.

16. EVERSTEIN F.C., STEVELS J.M. and WATERMAN H.I.,