EPR DETERMINATION OF THE POLARON ACTIVATION ENERGY IN CMR NANOPARTICLES

O.Raita1, M.N.Grecu2, D.Toloman1, X.Filip1, L.M.Giurgiu1, S.Idziak3and S.K.Hoffmann3

1National Institute for Research and  Development of Isotopic and Molecular Technologies, P.O. Box 700, R-400293,

Cluj-Napoca,Romania

2National Institute for Material Physics, 76900 Bucharest - Magurele,  P.O.Box MG-7, Romania

3National Institute for Molecular Physics, Poznan, Poland

We report an Electron Paramagnetic Resonance (EPR) investigation of the size effects in the paramagnetic regime of nanosized La0.67Ca0.33MnO3 manganites.

It is well established that the high-temperature conductivity in La0.67Ca0.33MnO3 is dominated by the adiabatic hopping motion of small polarons. We have evaluated the corresponding activation energy, Ea, from the temperature dependence analysis of  both:

(i) integral intensity and (ii) linewidth. The values obtained by method (i) are larger than the corresponding ones by using the bottlenecked spin relaxation scenario (ii). We have observed a decrease of Ea as the grain size diminished. It could be accounted for by considering both the Mn4+ content and the influence of the outer shell of La0.67Ca0.33MnO3 nanoparticles [1]. The polaron activation energy decreases with increasing the Mn4+ content  (inner core contribution) while one would expect an increase of Ea due to the increased  disorder in the surface layer of the smaller grains. Since the overall effect is a decrease of Ea, the core contribution to Ea seems to be dominant.

[1] O. Raita, M.N. Greu, X. Filip, D. Toloman, L.M. Giurgiu, S. Idziak, S. K. Hoffmann, Procc. “21-th International RAMIS Conference on Radio and Microwave Spectroscopy”, Poznan, Poland, Ed. S. Waplak, p29, 2005